# FINISHES FOR WOODTURNING

By Jerry Schaible

The following formulas for finishes are compiled from various printed sources and

discussions. These are not listed in any order of preference and some are used for

woodturning and others are listed for furniture.

1. Greg Jensen finishes... 3 types, depending on type of turning project:

- Mike Mahoney Walnut Oil

B. Danish oil. He uses 4 to 6 coats of Danish oil to bring out the highlights. Water

could be used as the lubricant for sanding to the finer grits.

C. Shellac... 2 lb cut. Shellac Finish...Brings out the best grain enhancement.

Sand woodturning to 220 grit. Use 4 to 6 coats and let dry 5 minutes between

coats. Brush on first coat and wipe off excess. Let dry 5 minutes. Sand lightly and

apply second coat, and 5 minute dry time. Apply no. of coats desired....4 to 6 coats.

Use Abralon Sanding Pads from Mirka Corp. He uses 5 inch sanding pads and

cuts them into 4 quarters. When last coat is applied, sand with Abralon through the

following grits, 500-1000-2000, using mineral oil as the lubricant. Store pads in plastic

bags. Let dry for 24 hours and wax and buff with the Beall system.

2. Larry McCardel Finishes Buckeye Woodworkers and Woodturners

A. Lacquer Finish. Campbell brand, located at Hartville Hardware in qts, gallons

and spray can. Spray lightly and let dry between coats. First coat is a 50 / 50 mix for

a sealer. Spray on 4 to 6 coats. Let dry for 24 hours. Buff on buffing wheel.

B. Danish oil.....Sand project to 320. Apply Danish oil with rag then sand with 400 grit.

Apply 2 nd coat of Danish oil and wet sand with 800 grip. Apply 3rd coat and wetsand

with 1000 grit. Apply 4th coat and wetsand with 1200 grit. Always sand slurry into

wood and wipe dry before moving to next grit. Wax and Buff.

C.  Friction Finish……2 parts shellac, 1 part oil, 1 part alcohol.

3.Ellis Walentine…..French Polish…..1 part shellac, 1 part denatured alcohol, 1 part

boiled linseed oil

4. Joe Smith…Northcoast Woodturners…wetsand Danish oil to 320 or 400

grit,..Dry 24 to 48 hrs, Sand to 1200 grit….apply a coat of Minwax wax and then buff.

5. Lothar Baumann…oil /varnish finish: 3 parts polyurethane…2 parts boiled linseed

oil…2 parts mineral spirits. Use 2 to 3 coats……lightly sand 1st coat with 600 paper

6. Garrett Hack…wiping varnish: 1 part polyurethane /1 part boiled linseed oil /1 part

turpentine.    Apply 3 or 4 coats.

7. Chris Minick…Finish Chemist in Stillwater Minn:

Danish Oil Mix… 1 1/2 cups mineral spirits, .1 cup brushing varnish [polyurethane]… 1/4 cup of linseed oil.

8. Sam Maloof ….famous woodworker in Calif.

A. 1part satin polyurethane….1 part linseed oil…1 part tung oil.

B. 1 cup boiled linseed oil, ..1 cup oil varnish…1 cup mineral spirits. The more oil in the formula results in better wiping properties, but longer drying times and less protection.

9. Bill Lovelace….Southwest Bowls….

- Thin coat of Parks Lacquer (type of sanding  sealer)..apply even coats and

watch for drips….sand with 0000 steel wool.

B. Use Jasco Tung Oil[polymerized]…5 or 6 coats, …..let first coat dry for 24 hrs.,

then apply second coat. Use 0000 steel wool between coats.

10. Art Carpenter furniture finish. Pro furniture woodworker since 1948. 1/3 part

linseed oil, 1/3 part turpentine, 1/3 part varnish[polyurethane]…..

- Damp cloth and wipe down project to raise grain.

- Sand to 220 or 320 grit.

- Wipe one coat of Danish oil and let dry for 24 hrs.

4.    Wipe on varnish mixture listed above….12 to 15 coats for table tops…5-7 coats for chairs and legs.

5. Use 0000 steel wool or gray Scotch brand/ Brite pads to smooth out any reflective

glare.

11. San Diego Woodturners French Polish: 1 part denatured alcohol, 1 part boiled linseed oil, 1 part clear shellac. Shake bottle to mix ingredients, sand to 320 or 400 grit. Power lathe at slow speed and apply finish with a rag. Sand with fine mesh. Apply next coat until 2 to 4 coats have been applied. Apply paste wax and buff.

12. Bonnie Klein, finish for turnings…..equal parts of shellac, boiled linseed oil and

solvent alcohol or Shellac thinner. Apply with rag and buff.

13. David Ellsworth….woodturner. uses a tung oil product called Waterlox. After power sanding to 320 or hand sanding to 600 grit[ he claims equal performance], he soaks the exterior of the piece. If hollow vessel he will not coat the inside. Let soak into wood. As tung oil dries he adds more coats.  When both the oil and wood [if turned wet] are both dry, he will buff off the oil residue using tripoli or white diamond buffing compound with wheel spinning at 3500 rpm. The turnings exterior looks like there is no finish at all and leaves a very natural look of the wood.

14.  Bob Flexner Finishing specialist. Wiping Varnishes are simply varnishes [including

polyurethane] thinned with 2 or 3 parts of mineral spirits or paint thinner.

Common commercial names are Formby’s Tung Oil Finish, Gillespie Tung Oil Finish, Hopes

Tung Oil Varnish, Jasco Tung Oil, Waterlox Transparent, Val-Oil, McCloskey Tungseal,

and Seal-a-cell. You can make any wiping varnish by adding enough mineral spirits to

any varnish so it’s easy to apply with a cloth.

Oil/Varnish blends such as Danish oil and teak oil are simply a blend of straight oil[linseed oil or tung oil] and varnish. Common names are Watco Danish Oil, Deft Danish Oil, Minwax

Antique Oil. You can make your own by mixing one part linseed oil or tung oil with one part of varnish. If mixture is to thick, then thin with mineral spirits.

Waterlox: 1 part polyurethane, 3 parts mineral spirits

Oil Varnish:1 part varnish, 1 part oil [any kind], 1 part mineral spirits

Wiping Varnish: 15% sanding sealer, 35% gloss lacquer, 50% lacquer thinner

Danish oil: 1 part varnish, 2 parts boiled linseed oil, 3 parts mineral spirits

Friction (French) Polish: 1 part denatured alcohol, 1 part shellac, 1 part boiled linseed oil